## Slide 1: Replacing Dimethicone as a binder in pressed powders with vegetable-derived alternatives
Diogo Baltazar, Elise Velkeneers and Slobodanka Tamburic
Cosmetic Science Research Group, London College of Fashion, London, UK

## Slide 2: Introduction and Aim
Growing consumer scepticism regarding silicones has prompted the of demand silicone-free products formulated with materials from natural and sustainable sources;
The industry has extracted and refined natural vegetable-based emollients as alternatives, but there is a lack of comparative data in the literature.
Aim of this project:
To evaluate the use of sustainable, vegetable-derived binders in pressed powders against a silicone standard, via an inter-and intra-formulary study using different binders and press strengths.

## Slide 3: Materials
Base formulation ingredients:
  Talc, Methylparaben, Propylparaben
  Pigment: CI 77510 (Ferric Ferrocyanide; Prussian Blue; Iron Blue)
Binders
  Dimethicone (DM)
  Vegetable-based binders:
    Diisooctyl Succinate (DOS)
    Triheptanoin (TH)
    Heptyl Undecylenate (HU)
DOS
TH
HU
Fig. 1 Molecular structure of vegetable-based binders

## Slide 4: Methods: formulation
Phase A – milling;
Phase B – add to Phase A + milling;
Bulk powder left to stand for 24 h;
Pressing @ 1000 or 2000 psi
Phase | INCI | % (w/w)
A | Talc | Ad 100%
 | CI 77510 | 10.00
 | Methylparaben | 0.20
 | Propylparaben | 0.10
Binder variables: |  | 
B | Dimethicone | 3.0 - 6.0 - 9.0
 | Diisooctyl Succinate | 3.0 - 6.0 - 9.0
 | Triheptanoin | 3.0 - 6.0 - 9.0
 | Heptyl Undecylenate | 3.0 - 6.0 - 9.0
Table 1. Pressed powder formulations

## Slide 5: Methods: testing bulk powder and colour
Bulk powder testing to characterise powder flow and compressibility, according to the British Pharmacopoeia:
  Aerated and tapped bulk densities (to obtain Hausner ratio and Carr index); Angle of repose.
Colour (L* a* b*), spectrophotometer, Konica Minolta;
  Variation:
Stability testing:
  Accelerated: 40º C, 10 weeks; followed by
  Indirect sunlight: RT, 10 weeks; followed by
  Xenon weathering: 765 W/m2, 24 h; followed by , adapted from L’Oréal’s QAC-MC-151 standard.

## Slide 6: Methods: testing compact powder
Drop test: 30 cm drop onto a flat surface, 3 times; adapted from ASTM D5276;
Hardness: 2 mm probe with a TA.XTplus Texture Analyser (Stable Micro Systems, UK); Eyeshadow Test Protocol and using the Exponent software.
Payoff – new method:
  Weighing, followed by testing:
    TA.XTplus Texture Analyser;
    Lipstick cantilever rig;
    Makeup brush;
  10 passes, followed by weighing.
Fig. 2 Payoff method with a cantilever rig on the TA.XTplus

## Slide 7: Results – vs formulation variables
Pressed Powder | ΔE 1000 vs 2000 psi
Benchmark | 0.25
DOS 3% | 2.86
DOS 6% | 2.00
DOS 9% | 2.35
DM 3% | 0.50
DM 6% | 0.35
DM 9% | 2.19
HU 3% | 1.98
HU 6% | 2.00
HU 9% | 4.21
TH 3% | 0.67
TH 6% | 0.69
TH 9% | 1.99
DOS, TH and HU increased Hausner ratio/Carr’s index and powder flow properties, thus performing better than DM.
over 2.5 is considered a visible difference to the human eye;
was high between samples with DM and those with vegetable-based binders – the latter gave higher colour intensity.
Fig. 3 between powders with same binder at different concentrations
Table 2. between press strengths

## Slide 8: Results – vs stability testing
Samples with DM consistently showed a high when compared to samples with vegetable-based binders, especially at higher binder concentrations.
Pressed Powder | 1000 psi | 2000 psi
Benchmark | 1.16 | 0.47
DOS 3% | 1.62 | 0.69
DOS 6% | 0.83 | 0.50
DOS 9% | 1.22 | 1.14
DM 3% | 1.00 | 1.64
DM 6% | 3.62 | 2.05
DM 9% | 10.18 | 9.86
HU 3% | 2.49 | 1.34
HU 6% | 2.41 | 1.79
HU 9% | 1.62 | 1.30
TH 3% | 2.14 | 1.21
TH 6% | 0.51 | 1.13
TH 9% | 1.20 | 0.86
Pressed Powder | 1000 psi | 2000 psi
Benchmark | 0.18 | 0.26
DOS 3% | 0.19 | 0.17
DOS 6% | 0.43 | 0.28
DOS 9% | 0.39 | 0.60
DM 3% | 0.67 | 0.70
DM 6% | 3.31 | 3.31
DM 9% | 10.00 | 10.85
HU 3% | 0.45 | 0.33
HU 6% | 0.66 | 0.71
HU 9% | 1.45 | 1.46
TH 3% | 0.89 | 0.25
TH 6% | 0.22 | 0.27
TH 9% | 0.72 | 0.56
Pressed Powder | 1000 psi | 2000 psi
Benchmark | 0.66 | 0.93
DOS 3% | 1.77 | 0.77
DOS 6% | 1.65 | 0.58
DOS 9% | 0.26 | 0.92
DM 3% | 0.97 | 1.82
DM 6% | 2.50 | 2.81
DM 9% | 10.15 | 10.27
HU 3% | 1.37 | 1.48
HU 6% | 1.57 | 0.98
HU 9% | 0.38 | 0.83
TH 3% | 0.57 | 0.50
TH 6% | 0.93 | 0.58
TH 9% | 1.46 | 0.43
Table 5. after 10 weeks, indirect light, RT
Table 4. after 10 weeks, accelerated stability (40º C)
Table 3. after 24 h, Xenon weathering

## Slide 9: Results – Drop Test
Pressed Powder | 1000 psi |  |  | 2000 psi |  | 
 | 1st Drop | 2nd Drop | 3rd Drop | 1st Drop | 2nd Drop | 3rd Drop
Benchmark | X | X | X | — | — | —
DOS 3% | — | — | — | O | — | —
DOS 6% | O | — | — | O | — | —
DOS 9% | O | O | — | O | O | O
DM 3% | X | X | X | O | — | —
DM 6% | O | — | — | O | O | —
DM 9% | O | O | O | O | O | O
HU 3% | O | O | — | O | O | O
HU 6% | O | O | — | O | O | O
HU 9% | O | O | O | O | O | O
TH 3% | O | — | — | O | O | O
TH 6% | O | O | O | O | O | O
TH 9% | O | O | O | O | O | O
Table 6. Integrity of pressed powders after 1, 2 and 3 drops, where ‘X’ indicates unacceptable damage (i.e. the pressed powder broke or cracked), ‘—' indicates minor damage (i.e. the pressed powder showed chipping), and ‘O’ indicates no damage
All binders increased compact resilience, except DM at 3% and 1000 psi.

## Slide 10: Results – Hardness
Fig. 4 Hardness (g) of pressed powders at different binder concentrations and press strengths
Samples with DM showed lower hardness compared to the vegetable-based alternatives at all binder concentrations and press strengths. This is in line with the drop test.

## Slide 11: Results – Payoff
Fig. 5 Payoff (% weight reduction) of pressed powders at different binder concentrations and press strengths
DM gave higher payoff (lower weight reduction), which is in line with both the hardness and drop test results;
Vegetable alternatives had similar payoff – consumer acceptability should be tested to confirm appropriateness.

## Slide 12: Conclusions
Vegetable binder alternatives provided, compared to DM:
  Better powder properties for compaction;
  Higher colour intensity and acceptable colour stability;
  Good properties in terms of compact powder hardness, integrity and payoff;
DM probably degrades under the test conditions;
Alternatives to DM potentially could be used at lower concentrations, making products more cost-effective;
Consumer acceptability should be considered in the future;
Vegetable-derived binder alternatives can perform better than DM and are in line with consumers’ preference for naturally-sourced sustainable alternatives to silicones.

## Slide 13
References
Mintel, Human ethics can boost palm oil’s profile (2018)
Mintel, Natural, Organic and Ethical Toiletries – UK (2017)
British Pharmacopoeia, Stationery Office (2014)
L’Óreal QAC-MC-151
ASTM D5276
E. F. C. Griessbach, R. G. Lehmann, Chemosphere, 38(6), 1461-1468 (1999)